# Direct cyclodextrin based powder extrusion 3D printing of budesonide loaded mini-tablets for the treatment of eosinophilic colitis in paediatric patients

Monica Pistone1; Giuseppe Francesco Racaniello1; Rosanna Rizzi2; Rosa Maria Iacobazzi1; Ilaria Arduino1; Antonio Lopalco1; Angela Assunta Lopedota1*; Nunzio Denora1*.

1 Department of Pharmacy – Pharmaceutical Sciences, University of Bari Aldo Moro, Orabona St. 4, 70125 - Bari, Italy.

2  Institute of Crystallography-CNR, Amendola St. 122/o, 70126 – Bari, Italy.

## *Corresponding authors: Prof. Nunzio Denora  e-mail: nunzio.denora@uniba.it; Prof. Angela Lopedota e-mail: angelaassunta.lopedota@uniba.it

## Abstract

The purpose of this study was to combine direct powder extrusion (DPE) 3D printing and fluid bed coating techniques to create a budesonide (BD) loaded solid oral formulations for the treatment of eosinophilic colitis (EC) in paediatric patients. The preferred medication for EC treatment is BD, which has drawbacks due to its poor water solubility and low absorption. Additionally, since commercially available medications for EC treatment are created and approved for adult patients, administering them to children sometimes requires an off-label use and an impromptu handling, which can result in therapeutic ineffectiveness. The DPE 3D approach was investigated to create Mini-Tablets (MTs) to suit the swallowing, palatability, and dose flexibility control requirements needed by paediatric patients. Additionally, DPE 3D and the inclusion of hydroxypropyl-β-cyclodextrin in the initial powder mixture allowed for an improvement in the solubility and rate of BD dissolution in aqueous medium. Then, to accomplish a site-specific drug release at the intestinal level, MTs were coated with a layer of Eudragit FS 30D, an enteric polymer responsive at pH>7.0 values. In vitro release experiments showed that film-coated MTs were suitable in terms of size and dose, enabling potential therapeutic customization and targeted delivery of BD to the colon.

## Keywords: Paediatric patients; Budesonide; Eosinophilic colitis; Direct Powder Extrusion; 3D Printing; Cyclodextrin.

## Introduction

Eosinophilic colitis (EC) is a rare disease characterized by elevated colonic infiltration of eosinophils in the absence of other causes of eosinophilia (Wang et al., 2021). EC is included in the Gastrointestinal Eosinophilic Diseases (EGID), first described by Kaijser in 1937, and recognized only in the last decade as a rare disease (Alfadda et al., 2011). The clinical scenario associated with this condition appears to be closely related to the layer of the affected intestine (Lozinsky and Morais, 2014), leading to abdominal pain, diarrhea, hematochezia, and bloating, while in rarer cases dysphagia, hypoalbuminemia, protein-loss enteropathy, and growth retardation may occur, especially in children and adolescents (Fang et al., 2019). The EC etiology is still not entirely clear (Wang et al., 2021) and, probably, the noticed increase in the eosinophilic population could depend both on genetic and environmental factors and predisposition to allergic reactions (Impellizzeri et al., 2019). Numerous studies reported that eosinophilic disorders in the colon can involve patients of all age groups, although a high incidence in the paediatric population has been observed (Guajardo et al., 2002; Melton et al., 2011). Specifically though, children representing a highly vulnerable patient category that requires considerable attention in identifying a specific treatment (Zuccari et al., 2022). Indeed, the paediatric age covers various groups, from newborns to adolescents, each characterized by precise physiological conditions, specific needs (Dimitri et al., 2021; El Aita et al., 2020) and continuous physical changes that require constant development and adaptation of drug therapies (Kearns et al., 2003). To date, there is no standard optimal treatment for EC (Wang et al., 2021). Initially, dietary therapies, such as the elimination diet or amino acid diet, are tried, which may have variable success depending on the severity of the disease (Lucendo et al., 2015). In cases of dietary treatment failure or extremely complicated and severe EC, corticosteroids are the first-choice therapy (Licari et al., 2019), despite having numerous systemic adverse effects after oral absorption (Magro et al., 2020). Budesonide (BD), a potent second-generation glucocorticoid, overcomes the limitations associated with its class due to extensive first-pass hepatic metabolism, which reduced its systemic toxicity (Herbada et al., 2021). Good local anti-inflammatory action and reduced systemic side effects make BD the drug of choice for the treatment of inflammatory bowel diseases (Yan et al., 2019). However, it is classified as a class II drug in the Biopharmaceutical Classification System (BCS), being described by specific physico-chemical characteristics, such as poor solubility in an aqueous environment, which limit its use (Laquintana et al., 2019). In addition, the action of BD in the distal intestine, and especially in the colon, is limited by the small amount of drug that reaches these areas (about 30 % of the administered dose), due to the high absorption that occurs as early as the initial tracts of the small intestine (Herbada et al., 2021). Therefore, for the treatment of EC, an oral BD-based formulation that could provide a selective and sustained colonic release and improve the physico-chemical properties of the loaded drug would be required. Several oral BD medicines, such as tablets and capsules, are commercially available (Gareb et al., 2019), which exploit different approaches to ensure site-specific colon release, using for example pH, and time sensitive polymers (Moghimipour et al., 2018). However, all commercial formulations are designed for adult patients and do not satisfy the needs of the paediatric population. Hence, to ensure therapeutic care for the paediatric patient group, many drugs are usually used “off-label”, and extemporaneous manipulation of marketed medicines is often required to achieve a suitable paediatric dose and/or to adapt the formulation to the appropriate route of administration for the specific age group (Zuccari et al., 2022), which may adversely affect drug bioavailability and therapy outcomes (Fang et al., 2019; Lafeber et al., 2022). For the above, is evident an unmet medical need in the paediatric population, which could be addressed with the development of oral formulations characterised by accurate and flexible dosages, sizes, and shapes suitable for swallowability in children, and with a specific selection of excipients (Lafeber et al., 2022).

Three-dimensional printing (3DP) is one of the most innovative techniques that can satisfy the needs of paediatric patients, ensuring to overcome the "one-size-fits-all" medicine by developing personalized medicine (Zema et al., 2017). This technique is based on the production of an object obtained by a gradual layering of material from a digital model. The use of computer-aided design (CAD) allows the object to be easily modified and make user-friendly. Numerous studies are reported in the literature involving the application of different printing techniques to obtain pharmaceutical dosage forms for paediatric use characterized by high flexibility in dosage, shape, drug release kinetics, and polymer composition (Boniatti et al., 2021; El Aita et al., 2020; Scoutaris et al., 2018). Among these, extrusion techniques appear to be the most widely utilized due to their versatility. Especially Direct Powder Extrusion (DPE) represents an innovative 3DP technique capable of directly extruding mixtures of excipients and active pharmaceutical ingredients (Goyanes et al., 2019; Pistone et al., 2022) overcoming the limitations associated with previous extrusion techniques, such as Fused Deposition Modelling (FDM), which is constrained using filaments, as raw materials, that have to meet specific physical and mechanical characteristics (Pistone et al., 2022). In fact, DPE enables the production of finished and customized pharmaceutical dosage forms in a one-step procedure in the form of amorphous solid dispersions (ASD). ASD represent a strategy to induce increased water solubility of drugs, due to the high free energy that the amorphous form acquires compared to its crystalline counterpart (Wang et al., 2022). The surfaces of drug molecules in the amorphous state are easily wetted, allowing for improved solubility and dissolution rate, even for the most poorly soluble drugs (Wang et al., 2022).

The aim of this study was, therefore, to exploit the DPE printing technique to produce Mini-Tablets (MTs) containing approximately 1 mg of BD, a dose deemed therapeutically appropriate and functional to ensure the customization of EC treatment in the different age groups that distinguish the paediatric population (Fang et al., 2019). Indeed, MTs represent a widely accepted pharmaceutical form in the paediatric population, being eventually produced with diameters ranging from 1.5 mm to 10 mm, depending on the patient's degree of acceptability which is closely related to age (Lafeber et al., 2022). Moreover, through the printing step, the BD undergoes an amorphization process, increasing its solubility and bioavailability. Specifically, three different powder mixtures consisting of selected excipients were produced and studied to implement the physico-chemical characteristics and achieve a suitable release profile of BD. Particularly relevant is the choice of hydroxypropyl-β-cyclodextrin (HP-β-CD), reported in the literature to be able to form stable inclusion complexes with BD and to increase its solubility (Bandi et al., 2004; Laquintana et al., 2019; Michailidou et al., 2021; Page et al., 2016). In addition, since hydrophilic polymers are known to induce further stabilisation of a drug/cyclodextrin (CD) inclusion complex (Medarević et al., 2015; Patel and Vavia, 2008), hydroxypropyl methylcellulose (HPMC, Affinisol 15 LV), a cellulose derivative with functional thermal properties for the 3D printing process, was selected as carrier polymer. An adjuvant blend (AB), consisting of sodium bicarbonate, citric acid, and tartaric acid, was also included in the formulations to speed up the dissolution of the HPMC, which if too slow could induce recrystallisation of the drug in the gel layer (Takano et al., 2020). Finally, polyethylene glycol (PEG) 6000 selected for its plasticizing properties was introduced in the mixtures (Alhijjaj et al., 2016). Furthermore, to reduce the absorption of BD at the small intestine level and allow greater dose release at the colon level, the MTs were coated by Wurster technique with the Eudragit FS 30 D polymer, capable of inducing selective release at a pH ˃ 7.0. It is an anionic copolymer of methyl acrylate, methyl methacrylate, and methacrylic acid, widely recognized as the excipient of choice for selective colon delivery (Gao et al., 2006; Rabito et al., 2012).

Hence, the present study proposes the development of an oral solid formulation, namely a MT specifically designed for paediatric use that, as demonstrated by in vitro dissolution studies, could enable selective colonic release of BD.

## Materials and Methods

### Materials

Micronized Budesonide, HP-β-CD (molar substitution 0.88), and PEG 6000 were purchased from Farmalabor s.r.l. (Canosa di Puglia, Italy). The HPMC (Affinisol HPMC HME 15 LV) was donated by Colorcon (Harleysville, USA). Citric Acid, Tartaric Acid, Sodium Bicarbonate, Phosphate monobasic Potassium, Sodium Hydroxide, and Methanol (≥ 99.9) were purchased from Sigma-Aldrich-Merck (Milan, Italy). Triethyl citrate (CITROFOL® AI Pharma) was supplied by Jungbunzlauer (Wien, Austria). Talc was purchased by Imerys Talc Italy S.p.A.. Eudragit® FS 30 D was donated by Evonik AG (Germany). For the analysis, distilled water (conductivity of 18.2 MΩ.cm at 23 °C) was obtained by the purification system Milli-Q (Purelab DI, MK2) (Elga, High Wycombe, UK).

### Preparation of inclusion complex BD/HP-β-CD

The BD/HP-β-CD inclusion complex (IC) was prepared in a solid-state by freeze-drying (FD), according to a method previously adopted by Laquintana et al. (Laquintana et al., 2019). Briefly, equimolar amounts of BD and HP-β-CD were added to 50 mL of water and the resulting suspension was kept under constant agitation for three days in order to enable the IC formation. Subsequently, the suspension was filtered through 0.22 µm cellulose acetate filters (Millipore®), then frozen and lyophilized at a pressure of 0.0060 bar and a temperature of -50 °C (Lio 5P, Milan, Italy).

### Determination of the BD loading degree in the inclusion complex

The amount of BD loaded into IC was determined by high-pressure liquid chromatography (HPLC) analysis, using an Agilent 1260 Infinity quaternary LC system equipped with an Agilent variable wavelength UV detector, a Rheodyne injector (Rheodyne, model 7725i) fitted with a 20 µL loop, and OpenLAB CDS ChemStation software (Agilent, Santa Clara, CA). For evaluation, a Zorbax C18 column (150 mm × 4 mm; 5 µm particles) was eluted in isocratic mode with a mixture of methanol and a solution of 0.1% trifluoroacetic acid (TFA) in deionized water (70:30 v/v), constantly monitoring the eluent at 254 nm. A flow rate of 1 mL/min and a column temperature of 35 °C were utilized, resulting in the elution of the drug at a time of 15 min. The data analysis was processed using Agilent OpenLab LC software.

In the first step, a calibration curve was performed in the range of 0.000991 mg/mL-0.0991 mg/mL, and a linear plot (R2= 0.9999) was produced.

For quantitative analysis, samples were obtained by accurately weighing 100 mg of lyophilized product, which was then solubilized in 25 mL of deionized water and filtered through 0.22 µm cellulose acetate filters (Millipore®). Finally, the samples were injected into the HPLC, after appropriate dilution. The BD loading degree into the IC was determined from the area of the resulting peaks and expressed in terms of encapsulation efficiency (%EE) (Arduino et al., 2021), calculated using the following equation:

%EE=Amount of encapsulated BDAmount of BD initially added x 100

### Preparation of powder mixtures

Three powder mixtures (MixBD, MixBD-CD, and MixIC) containing the same drug quantitative percentage (0.59 % w/w) and different polymer ratios were prepared. An adjuvant blend, denoted AB, and consisting of citric acid/tartaric acid/sodium bicarbonate in a weight ratio of 1:2:3.4, was present in all mixtures. AB had been previously prepared and then combined with the other selected polymers for the composition of the mixtures. The salt and the two acids were carefully weighed, mixed with a mortar and pestle, placed in an oven at 37 °C, and finally stored in a desiccator until used. A cellulose derivative, Affinisol HPMC HME 15 LV, was selected as the carrier polymer of the three mixtures and PEG 6000 was incorporated as a plasticizer, due to their high miscibility in the ratios studied (Illiger et al., 2009). In addition, HP-β-CD was added in MixBD-CD as such and in MixIC as IC (achieved as described in section 2.2.), for its ability to induce an increase in the aqueous solubility of the drug (Laquintana et al., 2019). The powder mixtures prepared in accordance with the mixing ratios of the selected materials are described in Table 1.

The components of each mixture were accurately weighed and sieved using a 355 µm mesh sieve. This operation was performed three times to ensure the homogeneity of the powder sizes. Subsequently, the mixtures were placed for about 1 hour at 67 rpm inside the shaker-mixer Turbula® T2C (Willy A. Bachofen GmbH, Nidderau, Germany) to permit homogeneous distribution of the drug in the powder. Finally, the resulting mixtures were dried on a stove at 37 °C overnight.

### Table 1. Composition relative to 100 g of powder mixtures for printing.

|  | BD* |  | AB* | IC* | HP-β-CD* | PEG 6000* | HPMC* |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | % w/w |  |  |  |  |  |
| MixBD | 0.59 |  | 20.00 | / | / | 3.97 | 75.44 |
| MixBD-CD | 0.59 |  | 8.17 | / | 46.41 | 2.99 | 41.84 |
| MixIC | / |  | 8.17 | 47.00** | / | 2.99 | 41.84 |

### *BD= budesonide; AB= Adjuvant Blend consisting of citric acid/tartaric acid/sodium bicarbonate; IC= BD/HP-β-CD inclusion complex; HP-β-CD= hydroxypropyl-β-cyclodextrin; PEG 6000= polyethylene glycol 6000; HPMC= hydroxypropyl methylcellulose.

** The value corresponds to 0.59% w/w of BD.

### Design and manufacture of 3D Mini-Tablets by Direct Powder Extrusion

The resulting feed mixtures were placed into the hopper of the 3D ForMe printer (Farmalabor, Canosa, Italy), with a specific extruder for the direct use of powders as previously reported (Pistone et al., 2022). A cylindrical geometry with a diameter of 5 mm and a height of 4 mm was designed using the CAD software Fusion360 and then selected as a template for the MT. The realized design was transferred as a stereolithography file (.stl) to the 3D printer software, Ultimaker Cura (version 4.6.2), and converted into a G-Code file. The parameters set on the 3D MT G-Code file were as follows: Layer height 0.15 mm, High resolution with a brim, Top/Bottom Thickness 0.8 mm, Top/Bottom Pattern Zig Zag, Infill Density 70%, Infill Pattern Concentric, Printing Temperature 180 °C, Build Plate Temperature 60 °C, Flow 100%, Print Speed 5 mm/s, Number of shells 2, Layer height 0.2 mm.

The 3D ForMe printer was specifically manufactured to enable the direct extrusion of powders using an extruder, which had a design based on a single-screw HME (Fig. 1). The screw's rotational speed was regulated by the 3D printer's software and permitted the flow of powder from the hopper to the melting block, thus regulating the extrusion time. In addition, the used nozzle had a diameter of 0.4 mm and moved in three directions, enabling layer-by-layer production of the 3D objects.

The three mixtures were printed keeping all the parameters set on the software and described above unchanged. Thus, the extrusion of MixBD, MixBD-CD, and MixIC resulted in the formulations MT1, MT2, and MT3 respectively. Once the printing of each formulation was completed, the extruder was disassembled: the screw was removed and suitably cleaned while the heating block was separated from the nozzle underneath, which was responded to in specific washing solutions. This operation was constantly repeated to avoid cross-contamination between the studied mixtures.

A batch of 50 MTs per formulation was produced, and the time required to complete the print of each tablet was approximately 3 min.

<< Insert Fig. 1>>

### Characterization of the 3D Mini-Tablets

The Hitech Diamond digital gauge was used to measure the physical dimensions (diameter and thickness) of the 3D MT. The evaluation of the uniformity of weight for each formulation was carried out in accordance with the quality control guidelines for magistral preparations given in F.U. I. XII (F.U.I. XII Ed.a). Thus, approximately 10 MTs were randomly selected from every three batches and accurately weighed using an analytical balance (Radwag XA 82/220/2X). For each batch, the mean mass, standard deviation, and percentage deviation of the weight of a single MT from the mean mass were determined. The weight uniformity test was satisfied if all MTs were within the range of ± 10 % w/w deviation from the mean. Electrical scanning microscopy (SEM), operating at 20 kV, was used to examine the morphology of the MT obtained during the printing process (Hitachi TM 3000 Tabletop SEM). The mechanical properties of the MTs were assessed by measuring the hardness carried out with a conventional Erweka GmbH D-63150 durometer. Thus, an increasing force perpendicular to the plane was applied to approximately 10 MTs of each formulation until a fracture was formed on the surface of the samples, which was indicative of the total fracture force relative to the MT examined. The friability test was performed as required by F.U. I. XII for tablets with a unit mass less than or equal to 650 mg (F.U.I. XII Ed.b). Briefly, taking a number of whole MTs having a mass as close as possible to 6.5 g, these were carefully depulverized and weighed. Subsequently, they were placed inside the Erweka GmbH TA 100 friabilometer and rotated at 25 ± 1 rpm for 4 minutes. The recovered MTs were again depulverized and reweighed, in order to assess the weight difference expressed as a percentage. The friability test was performed on the MT of each formulation. Also, the disintegration test was conducted on each formulation, following the guidelines given in F.U.I. XII (F.U.I. XII Ed.c). The test was performed in a basket disintegrator (Erweka ZT3-1 Disintegration Tester), thermoregulated at 37 ± 1 °C. Placing the MTs inside the appropriate baskets, they were kept for two hours in an acid medium (HCl 0.1N) and then in a pH 6.8 buffer solution for one hour.

### Determination of loaded drug by HPLC

One MT of each formulation was dissolved within a volumetric flask (50 mL) with a mixture methanol: water in a ratio 70:30 and left stirring at room temperature until completely dissolved.  The samples were then filtered through 0.22 µm cellulose acetate filters and analysed by HPLC, using the same method described in Section 2.3. The analysis was performed on 10 MTs for each studied formulation.

### Solid state characterisation of 3D Mini-Tablets

The solid-state characterisation of MTs was conducted and compared with those of the pure drug, physical mixtures containing only the excipients, and physical mixtures containing both the excipients and the drug. They were studied by Fourier transform infrared spectroscopy (FT-IR), differential scanning calorimetry (DSC), and powder X-ray diffraction (PXRD).

For FT-IR analysis, KBr pellets (2% of the sample) were analysed by FT-IR 1600 Perkin Elmer spectrophotometer. Data were acquired between 4000 cm-1 and 400 cm-1. Thermal DSC analysis was performed using the Mettler Toledo DSC822 instrument, which used nitrogen at 50 mL/min as the purge gas. Indium was used as a blank control and as a standard for enthalpy and temperature calibration. Samples (5-10 mg) were placed in an aluminium pan of 40 ml capacity and 0.1 mm thickness, closed with perforated aluminium lids. Finally, they were heated at the rate of 5 °C/min from 25 to 280 °C. For PXRD analysis, the patterns were collected by using a Rigaku Rint2500 rotating Cu anode, working at 50 kV and 200 mA in Debye−Scherrer geometry. The diffractometer is equipped with an asymmetric Johansson Ge (111) crystal to select the monochromatic CuKα1 radiation (λ = 1.54056 Å) and the silicon strip Rigaku D/teX Ultra detector. The range from 5 to 100 (2) was collected with a 0.02 (2) step size and a counting time of 2 s/step. Each powder was introduced in a glass capillary of 0.5 mm in diameter and mounted on the axis of the goniometer. The capillary was rotated during the measurement to improve the randomization of the orientations of the individual crystallites to reduce the effect of possible preferred orientation.

### In Vitro Drug Release Studies on 3D Mini-Tablets

The impact of the different polymer compositions of the three mixtures on the release profile of BD was investigated using a dissolution test paddle apparatus (VK 7000). The analyses were conducted in triplicate, setting the paddle rotation speed at 100 rpm and the temperature of the vessels at 37 ± 2 °C. To simulate transit in fluids with different pH values characteristic of the gastrointestinal tract, the dissolution test was conducted in three simulation media (Mirdamadian et al., 2022; Thakral et al., 2011). The MTs were placed in 50 mL of 0.1 N HCl pH 1.2 as a simulation of a gastric pH condition for two hours, followed by two hours in 50 mL of phosphate-buffered saline pH 6.8 (F.U.I. XII Ed.d) as the pH value of the intestinal fluid. Finally, MTs were placed until completely dissolved in 50 mL of phosphate buffer pH 7.4 (F.U.I. XII Ed.d), used as a colonic-simulating pH fluid. During the dissolution test, 1 mL samples were taken every 30 min and then filtered through 0.22 µm cellulose acetate filters and analysed by HPLC to determine the BD concentration.

### Preparation of Polymer Coating Dispersions

Polymethacrylate-based copolymer, Eudragit® FS 30 D, was used for the colon targeting coating as an aqueous dispersion. The mixture coating composition is described in Table 2.

Table 2. Composition of the polymer mixture used as film coating.

| Function | Ingredient | %w/w | Dry substance (g) |
| --- | --- | --- | --- |
| Polymer | Eudragit® FS 30 D | 43.01 | 12.9 |
| Plasticizer | Triethyl citrate | 0.65 | 0.65 |
| Anti-tacking | Talc | 6.45 | 6.45 |
| Diluent | Purified water | 49.89 |  |
| Total |  | 100.0 | 20.0 |

The coating suspension was prepared by adding talc and triethyl citrate in 49.89 g of water under continuous stirring for 10 minutes. Then, 43.01 g of dispersion of Eudragit® FS 30 D was added gently to the previous suspension prepared while stirring. The spray suspension was filtered through a 0.5 mm sieve and was maintained in stirring conditions during the process.

### Coating procedure

Among the three printed formulations, Mini-Tablet2 (MT2), obtained by direct extrusion of MixBD-CD mixtures, was evaluated as suitable to undergo the coating process. Therefore, MT2 was selected to evaluate the effectiveness and efficiency of both the coating process and the identified polymer blend (Table 2). The coating trial was performed using 600 g starting cores in a Glatt GPCG-2 6″ Wurster fluidised laboratory coater (Glatt GmbH, Germany). The process parameters set were inlet air temperature 35-45 °C, product temperature 25-28 °C, air flow rate 170 m3/h, atomising pressure 2.0 bar and spraying speed 5-7 g/min. The coating process was stopped when weight increments of 4% and 6% were reached. Thus, two different batches of coated MT2 (C-MT2) were obtained, denominated C-MT2 4% and C-MT2 6% according to the obtained weight gain.

### Characterization of coated MT2

The homogeneous surface distribution of the coating film carried out on C-MT2 (4% and 6%) was assessed using a Chemical Microanalysis investigation. The analysis was conducted with an optical stereomicroscope (SEM Hitachi TM 3000), equipped with a low-vacuum observation chamber, and the acquired images were elaborated using the Oxford Instruments SwiftED3000 for Hitachi TM3000 program. Briefly, the investigation was performed using a high-energy electron beam, denoted as Backscattered Electrons (BSE), capable of emitting radiation measured through an Energy Dispersive Detector (EDS). EDS microanalysis was combined with colourSEM technology through SEM-EDS. Thus, from the detected BSE image it was possible to observe the variation of the average atomic number on the sample surface and to obtain compositional and chemical information about the sample. In detail, microanalysis was used to assess the presence of the elements Si and Mg, which are characteristic of talc and thus only present in the coating suspension. Morphological analysis of C-MT2 4% and 6% were also conducted by SEM HITACHI TM3000 with DEBEN "Tilt & Rotate Sub-Stage," setting the accelerating voltage at 15 Kv, the vacuum values at 5x10-3 Pa and the working distance at 6.60 mm. Before analysis, the samples had undergone a metallization process with Au/Pd using an EDWARDS S150A Sputter Coater, placing them at vacuum values of 10-1 Pa and a voltage of 20 mA for two minutes. Finally, for the evaluation of the efficiency of the coatings process, a disintegration test was conducted as reported in Section 2.6, changing only the pH value of the basic medium, which shifted from 6.8 to 7.4.

### In vitro release studies on coated MT2

To estimate the efficiency of the filming process and the effectiveness of the used coating suspension, BD release studies were performed for C-MT2 4% and C-MT2 6% in the paddle dissolver previously described. The experiment was conducted in the same conditions reported in section 2.9. At predefined time intervals (30 min), 1 mL samples were taken and replaced with the same volume of pre-warmed fresh medium. The recovered samples were filtered through 0.22 µm cellulose acetate filters and finally analysed by HPLC.

### Statistical analysis

The experimental data were reported as mean ± standard deviation (SD). Statistical analysis was conducted by Graph Prism version 8.0.2 (Graphad Sofware Inc., La Jolla, CA, USA). Groups of data were calculated using a one-way analysis of variance (ANOVA) followed by the Bonferroni post hoc test, set at the probabilities of **** p<0.0001.

## Results and discussion

### Determination of the BD loading degree in the inclusion complex

Studies on BD complexation with HP-β-CD (IC) were widely reported in the literature, describing the formation of a hydrosoluble complex with a host (BD): guest (HP-β-CD) stoichiometry of 1:1 (Dufour et al., 2015; Kinnarinen et al., 2003; Laquintana et al., 2019; Santos Akkari et al., 2016). This IC was classified as an AL-type complex, according to the Higuchi-Connors model, and exhibited a typical pattern of the complex with 1:1 stoichiometry when studied by Job's diagram (Laquintana et al., 2019). As reported in the experimental section, the IC was produced by FD, which allowed the production of a high quality and homogeneous powder product (Ozdemir et al., 2018). The complexed drug content was assessed by HPLC analysis and the EE% was found to be 95.87%. The high efficiency demonstrated that the method selected for the realization of the IC provided excellent contact conditions between host and guest (Santos et al., 2015).

### Printing process by Direct Powder Extrusion

The main objective of this project was to obtain a pharmaceutical form that would provide flexibility control and dose customization and have an appropriate shape and size to meet the needs of vulnerable and inhomogeneous pediatric patients with EC. Specifically, BD-based MTs with different polymeric compositions were printed to select the best formulation. Thus, a cylindrical geometry of 5 mm in diameter and 4 mm in thickness was selected in the CAD design of the MT, as it was considered effective for overcoming the swallowability problem in children, compared to conventional tablets (El Aita et al., 2020b; Sánchez-Guirales et al., 2021; Suárez-González et al., 2021). The studied powder mixtures were alternately placed inside the hopper of the 3D ForMe printer, a single-screw extruder specified for the 3D DPE technique (Fig. 1). The three prepared powder mixtures resulted in a valid feed material for the 3D ForMe printer, permitting the set printing parameters to be maintained. This indicates that the choice of each excipient and their ratios were done correctly and permitted the formation of a fused mixture suitable for the extrusion process by DPE. All MTs were printed in the presence of AB, which is known to possess high sensitivity to temperature and humidity found both in external environmental conditions (Sun et al., 2020) and during the production of MTs (Lima et al., 2020). Moreover, loss of water from HP-β-CD, which is present in high amounts in MixBD-CD and MixIC, could wet the processed powder mixtures, turning them into a paste that is difficult to extrude (Pistone et al., 2022). These problems were overcome through the careful selection of other excipients. In particular, HPMC, in a grade with specific thermal properties optimized for the printing process, namely Affinisol HME 15 LV (Takano et al., 2020), and PEG 6000, as an appropriate plasticizer and glycating agent (Alhijjaj et al., 2016), were used, allowing the generation of powder blends with excellent fluidity and low hygroscopicity. Only MixIC exhibited slight extrudability problems, which required changing the printing and bed temperatures to 190 °C and 65 °C, respectively. This change was due to the presence in MixIC of the IC obtained by FD. Indeed, it has been widely reported in the literature that the FD process involves the formation of porous powders as a result of sublimation of ice crystals under vacuum (Liao et al., 2020). The porosity of the powders induces an increase in the contact surface, which in turn leads to a reduction in the tendency to slip (Liu et al., 2020). For this reason, the fluidity of MixIC inside the 3D ForMe's extruder reduced compared to other blends, and consequently, its extrusion required slight temperature adjustments to allow its respective MT to print. The time needed to print a single MT was about three minutes, thus in one hour, it was possible to print a consistent number of MTs for patient therapy. The printed MTs loaded with BD and relative to the three formulations (here in after MT1, MT2, and MT3), were of a pale-yellow color and well defined shape due to the high adhesion between layers, as shown in Fig. 2.

DPE, the most innovative 3D printing technique, appears more efficient in terms of dosing flexibility, time, and number of steps than the other conventional techniques applied for the development of MTs for paediatric use (Lafeber et al., 2022). Indeed, several other approaches are reported in the literature, including Direct Compression (DC) and Electrospinning Technique (ET). While the DC method results practical and fast for production, it presents a major limitation in the dosage selection of active ingredients. In fact, large percentages of poorly compressible actives do not provide tablets with acceptable hardness, and low amounts of actives do not provide adequate homogeneity of the mixture (Zhao et al., 2018; Zuccari et al., 2022). In contrast, the ET presents the process scalability as a major limiting factor due to the high production time, despite allowing the production of nanofibres customised in diameter (nm, µm) and release, characteristics requested in paediatric drug design (El-Say et al., 2015; Poller et al., 2017). Moreover, DPE overcomes the limitations associated with other most commonly used 3D printing techniques, such as FDM (Boniatti et al., 2021; Pistone et al., 2022). In fact, the elimination of the intermediate Hot Melt Extrusion (HME) filament production required by the FDM technique, allows DPE to expand the selection of excipients and active ingredients and speed up the process (Pistone et al., 2022). These advantages facilitate the application of DPE in daily galenic practice to achieve patient-centered therapies.

<< Insert Fig. 2>>

### Characterization of 3D Mini-Tablets

The values of weight, drug content, friability, breaking force, and dimensions of the three different printed MTs formulations were given in Table 3. As reported in the literature, the accuracy of the DPE printing process results in MT with high dimensional reproducibility of the CAD design (Pistone et al., 2022; Sánchez-Guirales et al., 2021). In fact, the average diameter of printed MT was between 5.17 mm and 5.52 mm (G-code set at 5 mm) and the average height ranged from 3.76 mm to 4.14 mm (G-code set at 4 mm). A high level of repeatability of the DPE process was also confirmed by the low variation in weight of the three different MTs, ranging from 127.08 mg to 130.40 mg. This allowed all formulations to satisfy the weight uniformity test, with weight within the deviation range from the mean value specified by F.U.I. XII (± 10%) (F.U.I. XII Ed.a). The MTs showed also acceptable friability values (< 1%) (F.U.I. XII Ed.b) and sufficiently high hardness properties to warrant packaging and handling operations. These were the results that could have been expected for MTs obtained by a 3D printing process involving the fusion and subsequent solidification into compact layers of a polymer matrix. In fact, the 3D formulations usually have lower friability and higher hardness when compared with tablets achieved by conventional direct compression procedures (Kuźmińska et al., 2021). Moreover, the difference in breaking force values found between MT1 and the other formulations could be explained by the different compositions of the mixtures. Indeed, in the MixBD, the % w/w of the HPMC was the highest among the blends and the cyclodextrin (CD) was completely absent. This may have led to increased compaction of the molten mixture consisting mainly of one polymer. The content uniformity test allowed the evaluation of the amount of BD loaded in the MTs which was found to be highly comparable between the MT1 and MT2 formulations. Instead, MT3 had a lower amount of drug, mainly related to the %EE of the IC obtained by FD, which was about 96%, as reported in Section 3.1. In fact, to keep unchanged the mixing ratios of the polymers studied in MixBD-CD, the total % (w/w) of IC present in MixIC matched with the sum of the % (w/w) of BD and HP-β-CD in MixBD-CD. The study of these mixtures also allowed to highlight any differences between the IC obtained by the two different techniques, DPE and FD.

Table 3. For each formulation, the characteristics of each MT obtained by DPE.

| MT | Weight Uniformity* (mg) | Drug content* (mg) | Friability* (%) | Breaking Force (N)* | Dimensions (mm)* |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Diameter | Height |
| 1 | 128.08 ± 20.17 | 0.71 ± 0.09 | 0.022 | ˃ 484.00 | 5.17 ± 0.29 | 4.14 ± 0.33 |
| 2 | 127.08 ± 10.68 | 0.68 ± 0.09 | 0.064 | 298.67 ± 62.14 | 5.52 ± 0.21 | 3.78 ± 0.13 |
| 3 | 130.40 ± 18.39 | 0.60 ± 0.05 | 0.038 | 320.08 ± 97.70 | 5.46 ± 0.18 | 3.76 ± 0.21 |

* The value is the average of 10 tablets. ± is the deviation standard.

In addition, MT1, MT2, and MT3, produced by the DPE printing technique, satisfied the gastro-resistant solid form disintegration assay (F.U.I. XII Ed.c). This was achieved thanks to the incorporation of the AB, consisting mainly of sodium bicarbonate, into the hydrophilic polymer matrix di HPMC (Xi et al., 2020).  In fact, for the latter, it is well documented in the literature that, when placed in contact with aqueous media, it tends to swell, erode by mechanical friction, and/or dissolve at different times dependent on both the conditions of the external aqueous environment and the physicochemical characteristics of the polymer (Maroni et al., 2016; Siepmann and Peppas, 2012). Among them, the hydration and viscosity properties play an important role in the disaggregation process as they induce the formation of a gel layer with a variable thickness (Maroni et al., 2016). Therefore, the HPMC is involved in slow disintegration due to its gel-forming nature that causes the formation of a very dense gel layer (Pistone et al., 2022). Kajiyama et al. reported that the disintegration of HPMC matrix tablets was faster and more efficient as a result of the inclusion of inorganic salts in their composition (Kajiyama et al., 2008). In fact, the salts influence the solubility of the polymer due to their dehydrating effect, denoted as “salting-out”, which allows them to compete with the polymer for interactions with water (Takano et al., 2020). The salts bind water, forming ordered hydric structures that induce the dehydration of the gel layer and the self-association of the polymer's hydrophobic chains (Takano et al., 2020). Among all inorganic salts, sodium bicarbonate, which is present in the AB component of the powder mixtures, possesses a high dehydrating power, which could depend partly on its ionic effect and also on its ability to generate carbon dioxide (CO2) in an acidic environment (HCl) (Xi et al., 2020). Moreover, bicarbonate effervescence improves in the presence of tartaric acid and citric acid (the other components of AB) (Pereira et al., 2017), and undergoes an additional enhancement when applied in conjunction with more common fusion techniques, such as HME (Alam et al., 2015; Lima et al., 2020). For these reasons, due to incorporation of AB, the HPMC-based MTs, obtained by the innovative DPE hot-melt technique, successfully satisfied the disaggregation assay, required by F.U.I., resulting in a reduction of polymer swelling and an increase in its solubility.

The 3D MTs images obtained by SEM showed a compact and uniform surface with a slight degree of roughness probably due to the inclusion of AB within all the formulations (Fig. 3, MT1(AI), MT2(BI), MT3(CI)). This was most evident in MT1 (AI) where the amount of AB present was significantly higher than in the other two formulations. In addition, the cross-sectional images of the MT revealed layers with a thickness of 0.2 mm that were perfectly fused and compacted with each other, which allowed faithfully reproduction of the cylindrical geometry set in the G-Code (Fig. 3, MT1(AII), MT2(BII), MT3(CII)).

<< Insert Fig. 3>>

### Solid state characterisation of 3D Mini-Tablets

The solid-state characterisation was carried out to evaluate the possible amorphisation process undergone by the drug during the extrusion phase. In order to have a comparison between the samples before and after the DPE printing stage, the results of FT-IR, DSC, and X-Ray analyses of the obtained printed formulations (MT1, MT2, MT3) were compared with those of the respective mixtures (MixBD, MixBD-CD, MixIC). For a more detailed investigation, analyses were also conducted on the sample of pure drug and the physical mixtures consisting of excipients alone (Mix1, Mix2/Mix3). A single spectrum was reported for the physical mixtures Mix2 and Mix3 because they presented the same polymer composition. In fact, these were mixtures used for MixBD-CD and MixIC, respectively, differentiated by the presence in powder of BD and HP-β-CD in the former case and an IC pre-formed by FD in the latter. The study on MixBD-CD and MixIC mixtures aimed at highlighting, through direct comparison with the IC obtained with FD, the possible formation of an IC during extrusion by DPE, as reported in our previous study with the same cyclodextrin and a different drug (Pistone et al., 2022).

From the FT-IR spectrum of BD, it was possible to observe the characteristic peaks of the drug present at 3499 cm-1 for the O-H stretching vibration, at 2955 cm-1 for the C-H stretching vibration, at 1722 cm-1 and 1670 cm-1 for the stretching vibrations of the carbonyl groups (C=O) of acetyl and dihydrobenzoquinone, respectively, and again at 1626 cm-1 for the stretching vibrations of the C=C bond (Mali et al., 2014) (Fig. 4). In contrast, the spectrum related to IC BD-CD, obtained by FD technique, showed that the intensity of the drug bands decreased and there was a shift in the elongation bands of the methyl groups from 2955 cm-1 to 3000 cm-1. These results suggested a rearrangement of the above-mentioned functional groups of BD as a result of possible interactions with HP-β-CD (Michailidou et al., 2021). Depending on the different compositions, in the FT-IR spectra of the medicated physical mixtures (MixBD, MixBD-CD, MixIC) and not (Mix1, Mix2/Mix3) were mainly evident the characteristic peaks of HPMC, as reported by Wang et al.  (Wang et al., 2022), and/or HP-β-CD, as reported by Yuan et al. (Yuan et al., 2015), the polymers being present in higher quantity. Finally, the significant peak deformations found in the samples of the extruded formulations (MT1, MT2, MT3) containing drug-hydrophilic polymer-cyclodextrin may be determined by the numerous interactions of BD with HPMC and/or HP-β-CD. Therefore, the absence of the peaks at 3490 cm-1 and 2950 cm-1 and the change in the carbonyl group rearrangement peculiar of BD, in combination with the enlargements of the HP-β-CD and HPMC peaks at 3350 cm-1 and 3460 cm-1 respectively, suggested that the extrusion process allowed the possible formation of a ternary inclusion complex (BD/CD/HPMC) (Granados et al., 2022; Thiry et al., 2017).

<< Insert Fig. 4>>

These intimate BD/CD/HPMC interactions were investigated with a second test performed by DSC (Fig. 5). As reported in previous studies, DSC analysis of BD showed an endothermic event corresponding to the melting of the drug at a temperature of 260 °C (Goyanes et al., 2015). The thermogram of the IC obtained by FD appeared amorphous, with a single sloping peak between 80 and 100 °C related to the removal of water present in the sample and characteristic of the CD molecules. This indicated the loss of the crystalline state and the acquisition of the amorphous one by BD, as a result of lyophilization and its inclusion within the hydrophobic cavity of HP-β-CD (Kim et al., 2014). In the physical drug-free mixtures, only endothermic events related to PEG 6000 and tartaric acid were observed, which were present at 60 °C and 173 °C, respectively (Altamimi and Neau, 2017; Pereira et al., 2017), both HPMC and CD being intrinsically amorphous polymers. In contrast, the absence of the BD melting peak in MixBD, MixBD-CD, and MixIC mixtures was found as a result of a potential in situ interaction between the drug and polymers that occurred during thermal analysis (Lima et al., 2020). In fact, since the glass transition temperatures of all the components were lower than the melting temperature of BD (55 °C, 115 °C, 120-180 °C, 157 °C, and 173 °C for PEG 6000, HMPC, sodium bicarbonate, citric acid, and tartaric acid, respectively), high polymer mobility was generated during heat treatment, which promoted drug interactions with the polymers (Saokham et al., 2020). The absence of the endothermic peak of BD in the thermograms of the printed formulations indicates the complete dispersion of the drug in amorphous form and its high compatibility with polymeric solid solutions (Granados et al., 2022). Thus, the demonstrated solubility of BD in the fused polymer mixture enabled the amorphization process of the drug and potentially generated a favourable condition for IC formation by DPE (Malaquias et al., 2018).

<< Insert Fig. 5>>

In Fig. 6, from top to bottom, the powder X-ray diffraction patterns of each component of the AB (Sodium Bicarbonate, Tartaric Acid, Citric Acid), the pure drug (BD), the physical mixtures without the drug (Mix1, Mix2/Mix3), the physical mixtures medicated (MixBD, MixBD-CD, MixIC) and the obtained extruded formulations (MT1, MT2, MT3), are reported. The crystallinity of the pure BD is underlined by the presence of sharp diffraction peaks, the intensity of which is reduced when the drug is inserted in Mix2/Mix3, as confirmed also by the FT-IR results. In terms of crystallinity, there are no evident differences between MixBD-CD and MixIC.

Conversely, the almost complete disappearance of peaks in the pattern of MT1, MT2, and MT3 clearly shows the BD amorphization during the printing phase. This phenomenon, already pointed out by FT-IR and DSC results is confirmed also by the PXRD analysis.

The few residual peaks still present in the formulations are attributable to AB and are of higher intensity in MT1 due to the highest AB concentration in it with respect to the other formulations.

<< Insert Fig. 6>>

### In vitro dissolution test of printed Mini-Tablets

BD release studies from formulations obtained by the DPE 3D printing process were conducted for eight hours, employing fluids with pH values simulating the gastro-intestinal tract. Formulations led to important changes in the properties of BD, concerning improvements in aqueous solubility and rate of dissolution compared to the pure drug. Indeed, BD as a crystalline and hydrophobic compound exhibited an in vitro dissolution capacity of up to 14 ± 1.5%, when placed in a pH 7.4 medium (data not shown). This result evidenced the high efficiency of the DPE printing process in achieving the one-step formation of solid dispersions in which the drug particles were molecularly dispersed (Boniatti et al., 2021; Pistone et al., 2022). The increase in surface area and the acquisition of the amorphous state of the drug were the main factors responsible for its increased dissolution (Soltani et al., 2022). All MT formulations released 100% of BD within the eight hours, however, showing differences in release profiles, as illustrated in Fig. 7. Specifically, MT1 exhibited a slower and more gradual release of the drug that was completed after three hours in the medium simulating the colonic pH environment (seven hours total), while MT2 and MT3 showed more rapid release that reached the totality of the loaded drug before reaching the colonic environment (after four hours). MT2 and MT3 showed an almost perfect overlap of their respective release profiles, confirming the formation of the IC via DPE (MT2) and its comparability with the IC obtained by FD (MT3). The observed differences in the dissolution curves of MT1 with MT2/MT3 depended on the polymeric composition of the matrix and mainly on the different concentrations of HPMC. It is well documented that HPMC is a polymer widely used for the development of oral sustained-release pharmaceutical forms due to its ability to swell after exposure to aqueous media that influences drug release kinetics (Palugan et al., 2021; Ribeiro et al., 2003).  In fact, when the polymer is hydrated, it generates a dense viscous layer on the tablet surface that limits both the mobility of incoming water and outgoing drug (Xi et al., 2020). As the polymer concentration increases, further gelling of the polymer could occur, inducing slow erosion of the tablet (Xi et al., 2020). As previously described in Section 3.3, the presence of AB in the composition of MTs has a major impact on the degree of hydration of the polymer resulting in a high influence on its rate of disaggregation and dissolution (Takano et al., 2020). This was also confirmed by release studies of MTs that showed how the presence of salts, such as sodium bicarbonate, dehydrates the HPMC and reduces swelling of the matrix consequently inducing faster diffusion of the drug from the formulation. Probably, in MT1 the high amount of HPMC generated a very thick and viscous layer that the salts could not counteract, slowing the drug release. Instead, in MT2 and MT3 formulations, the modulation of drug release also depended on the presence of HP-β-CD, which increased the aqueous solubility of BD and improved its diffusion from the swollen barrier of the HPMC (Bibby et al., 2000; Pose-Vilarnovo et al., 2004). Specifically, already after the first two hours, there was a significant difference in the amount of drug released from MT1 compared to the other formulations, 42 ± 2.5% in the first case and about 80 ± 4.1% for MT2 and MT3 (p <0.0001). Indeed, it is known that CD may be able to alter the hydrodynamic layer around drug molecules, inducing a rapid increase in dissolved drug concentration (Takano et al., 2020). Hence, the addition of HP-β-CD in the HPMC matrix showed a synergistic effect in inducing an increase in BD solubility, confirming numerous studies that had demonstrated that the sum of the individual solubility values related to CD and hydrophilic polymer was lower than the solubility found experimentally in the presence of both (Loftsson et al., 1999; Medarević et al., 2015; Ribeiro et al., 2003). Hydrophilic polymers, such as HPMC, stabilize the IC and implement complexation efficiency, allowing an improvement in some physico-chemical properties, such as solubility and dissolution rate (Medarević et al., 2015). A similar effect is also found after the incorporation of small amounts of low molecular weight compounds, such as amino acids, organic acids and bases (Aiassa et al., 2021). Thus, the presence of the hydroxycarboxylic acids of AB (citric acid and tartaric acid) could also enhance the interaction between BD and CD, performing the function of cross-linker between the two molecules (Londhe et al., 2020; Rakkaew et al., 2018). Indeed, citric acid and tartaric acid could form hydrogen bonds between the drug and the CD (Redenti et al., 2000), thanks to the presence of numerous hydrophilic groups in their structure, capable of causing an increase in the solubility and bioavailability of the drug (Barillaro et al., 2005; Jug et al., 2014).

The obtained results confirmed the amorphisation process undergone by the drug during DPE extrusion and suggested the formation of a multi-component complexation between BD/ HP-β-CD/ HPMC/ hydroxy acids. Both processes were desired to induce an improvement in the chemical and physical properties of BD.

<< Insert Fig. 7>>

It is necessary to consider that the dissolution test on the printed MTs was carried out in order to evaluate the formulation most able to improve the solubility and dissolution rate of BD and so as to increase its bioavailability to the colon once coated. From the obtained results, such a formulation was identified in MT2, which not only fulfilled its intended purpose, but also highlighted the capabilities of the DPE technique in inducing the formation of a BD/CD IC stabilized by HPMC and hydroxy acids.

### Characterisation of coated MT2

To enable modified, site-specific release at the colonic level, the strategy of exploiting local pH, which involved the use of pH-responsive polymers, was applied. Eudragit FS 30 D, an anionic copolymer of methyl acrylate, methyl methacrylate, and methacrylic acid, was selected for its ability to dissolve at pH=7.0, specific to the colonic environment (Huyghebaert et al., 2004). Eudragit FS 30 D, available as an aqueous dispersion with 30 % polymer content, had often been used as a coating polymer for enteric release (Letmanski et al., 2015; Moghimipour et al., 2018; Rabito et al., 2012). Due to its low minimum film-forming temperature (14 °C) and glass transition temperature (45 °C), Eudragit FS 30 D does not require the inclusion of high amounts of plasticizing agents (Huyghebaert et al., 2004), which are used in colloidal polymer suspensions to reduce process temperatures (Wesseling et al., 1999). In fact, optimal processing conditions could be achieved by the addition of only 0.65 % (w/w) of the plasticizer triethyl citrate. However, it was deemed appropriate to add an anti-adhesion agent in the coating suspension, identified in talc powder, that could inhibit the agglomeration of polymer particles and induce an acceleration of the process (Maejima and McGinity, 2001; Wu and McGinity, 2003). The importance of talc was mainly evident in aqueous-based coating suspensions, rather than in those based on organic solvents (El-Malah and Nazzal, 2008). Indeed, in aqueous systems, the phenomena of coalescence and interdiffusion of polymer particles occurred as a result of the evaporation process of water (El-Malah and Nazzal, 2008). The latter, combined with the high latent heat of vaporization, caused the stickiness of aqueous systems. Thus, the use of an anti-adhesion agent countered the high stickiness of aqueous systems.

The coating process resulted in two different batches of MT2 (C-MT2s) depending on the final weight gain found. In fact, MT2 with 4 % and 6 % coating were obtained (Fig. 8).

<< Insert Fig. 8>>

A chemical microanalysis was carried out on both batches aimed at detecting the Si and Mg elements, owned by the structure of talc, since it was present only in the coating suspension. As can be seen in Fig. 9, C-MT2 4% and C-MT2 6% were homogeneously coated given the uniform distribution of Si (in red) and Mg (in green) on the surface of the respective MT.

<< Insert Fig. 9>>

SEM images of the cross-section of the C-MT2s (4% and 6%) allowed the measurement of the thickness of the coating layer and its uniform distribution on the surface of the MTs. As expected, a greater percentage of coating (6%) corresponded to a greater thickness, which was found to be 265 µm. In contrast, in C-MT2 4% the thickness identified was 162 µm, as shown in Fig. 10.

<< Insert Fig. 10>>

The disintegration test was conducted following the guidelines provided for gastro-resistant tablets given in F.U.I. XII (F.U.I. XII Ed.c). Only one modification was made regarding the pH value of the basic medium used, which was 7.4, rather than 6.8 as required. This change was necessary to induce pH-responsive dissolution of Eudragit FS 30 D. Thus, the C-MT2s were placed first in an acidic medium (HCl 0.1 N, pH 1.2) for two hours and then in a basic medium (pH=7.4) for one hour. In particular, they remained intact and slightly swollen at the level of the core matrix after being in the acidic environment, in contrast, when replacement with the basic medium occurred, they began the disintegration process, as the coating film had started to dissolve. Therefore, based on the results of the conducted analysis, it was agreed that the coating film designed and applied on MT2 was effective in ensuring gastro-resistance and enabling site-specific release at the colonic level whether applied at 4 % or 6 %.

### In vitro release studies on coated MT2

The dissolution test was conducted on 4% and 6% C-MT2 in media with pH values simulating those of the gastrointestinal tract (in order: 1.2, 6.8, 7.4) to compare the efficiency of the coating applied to MT2 versus uncoated MT2. As can be seen in Fig. 11, C-MT2 4% after the first two hours in acidic medium (pH 1.2), induced BD release of about 10% and 30% after the next two hours in simulated enteric medium (pH 6.8). In contrast, C-MT2 6% released only 2% BD after passage in the first two media. In fact, C-MT2 4% already before reaching the simulated colonic fluid (pH 7.4) showed signs of erosion and dissolution of the film-forming coating, with partial swelling of the internal HPMC matrix (inset A, Fig. 11), while C-MT2 6% showed complete integrity of its coating that had prevented changes in the state of the hydrophilic core (inset B, Fig. 11). A very important factor that may have determined this difference between the two coated formulations was probably the thickness of the coating layer. In fact, in the literature, numerous studies highlight the influence of coating thickness on the regulation of drug release (Gao et al., 2006). Therefore, C-MT2 6% proved to be the most promising formulation for selective and specific colonic targeting due to the high thickness of its coating layer, which enabled it better to resist pH changes.

<< Insert Fig. 11>>

## Conclusions

In this study, we investigated innovative BD-loaded MTs produced by DPE 3D printing and fluid bed coating techniques. This strategy paves the way for flexible dosing formulations that, together with the shape and size of the final tablet, enable personalized therapy. This represents a need in the case of rare diseases and special categories of patients, such as children. Specifically, HPMC-based MTs were successfully developed and designed through the DPE 3D technique. The MTs showed good mechanical and physical properties, and to increase the dissolution rate and solubility of BD, multiple approaches involving the use of HP-β-CD and AB mixture, which can form inclusion complexes with BD and increase the disintegration of the MTs, was studied, respectively. All of the tested MTs improved the pure drug's dissolving profile. Among them MT2 stood out as the best one since it could be made in a single step that simultaneously produced the inclusion complex between BD/HP-β-CD and tablet printing. Then, MT2 was coated with an enteric polymer at different thicknesses, with the 6% coating proving to be the most effective. In fact, after being exposed to an acidic medium and subsequently to a buffered solution with a pH of 6.8, the 6% C-MT2 released just 2% of BD, essentially preserving the coating. As a result, such a formulation might be described as a possible response to EC treatment in paediatric patients.

Acknowledgements

The authors would like to thank Dr. Luca Donati, Dr. Danilo D'Amico and Dr. Alessandro Conte from the Pharma Formulation Development of Angelini Pharma S.p.A. for their assistance in film coating. Authors acknowledge Farmalabor s.r.l., Centro Studi e Ricerche “Dr. S. Fontana 1900-1982” for their technical support. The authors would like to thank Dr. Francesco Baldassarre and Dr. Pasquale Trotti for their contribution in the PXRD analysis and the SEM analysis, respectively. M.I.U.R- Programma Operativo Nazionale 2014-2020; Azione: l.1- Dottorati di ricerca innovativi 2020, M.I.U.R- Programma Operativo Nazionale 2014-2020 Green e Innovazione, and the University of Bari (Italy) are also gratefully acknowledged for the financial support.

Funding

M.I.U.R- Programma Operativo Nazionale 2014-2020; Azione: l.1- Dottorati di ricerca innovativi 2020.

## References

Aiassa, V., Garnero, C., Longhi, M.R., Zoppi, A., 2021. Cyclodextrin multicomponent complexes: Pharmaceutical applications. Pharmaceutics 13. https://doi.org/10.3390/pharmaceutics13071099

Alam, M.A., Al-Jenoobi, F.I., Al-Mohizea, A.M., Ali, R., 2015. Effervescence Assisted Fusion Technique to Enhance the Solubility of Drugs. AAPS PharmSciTech 16, 1487–1494. https://doi.org/10.1208/s12249-015-0381-2

Alfadda, A.A., Storr, M.A., Shaffer, E.A., 2011. Eosinophilic colitis: An update on pathophysiology and treatment. British Medical Bulletin 100, 59–72. https://doi.org/10.1093/bmb/ldr045

Alhijjaj, M., Belton, P., Qi, S., 2016. An investigation into the use of polymer blends to improve the printability of and regulate drug release from pharmaceutical solid dispersions prepared via fused deposition modeling (FDM) 3D printing. European Journal of Pharmaceutics and Biopharmaceutics 108, 111–125. https://doi.org/10.1016/j.ejpb.2016.08.016

Altamimi, M.A., Neau, S.H., 2017. Investigation of the in vitro performance difference of drug-Soluplus® and drug-PEG 6000 dispersions when prepared using spray drying or lyophilization. Saudi Pharmaceutical Journal 25, 419–439. https://doi.org/10.1016/j.jsps.2016.09.013

Arduino, I., Liu, Z., Iacobazzi, R.M., Lopedota, A.A., Lopalco, A., Cutrignelli, A., Laquintana, V., Porcelli, L., Azzariti, A., Franco, M., Santos, H.A., Denora, N., 2021. Microfluidic preparation and in vitro evaluation of iRGD-functionalized solid lipid nanoparticles for targeted delivery of paclitaxel to tumor cells. Int. J. Pharm. 610. https://doi.org/10.1016/j.ijpharm.2021.121246

Bandi, N., Wei, W., Roberts, C.B., Kotra, L.P., Kompella, U.B., 2004. Preparation of budesonide- and indomethacin-hydroxypropyl-beta-cyclodextrin (HPBCD) complexes using a single-step, organic-solvent-free supercritical fluid process. Eur J Pharm Sci 23, 159–168. https://doi.org/10.1016/j.ejps.2004.06.007

Barillaro, V., Evrard, B., Delattre, L., Piel, G., 2005. Oral bioavailability in pigs of a miconazoleγ/hydroxypropyl-γ-cyclodextrin/L-tartaric acid inclusion complex produced by supercritical carbon dioxide processing. AAPS Journal 7. https://doi.org/10.1208/aapsj070116

Bibby, D.C., Davies, N.M., Tucker, I.G., 2000. Mechanisms by which cyclodextrins modify drug release from polymeric drug delivery systems. International Journal of Pharmaceutics 197, 1–11. https://doi.org/10.1016/S0378-5173(00)00335-5

Boniatti, J., Januskaite, P., da Fonseca, L.B., Viçosa, A.L., Amendoeira, F.C., Tuleu, C., Basit, A.W., Goyanes, A., Ré, M.I., 2021. Direct powder extrusion 3d printing of praziquantel to overcome neglected disease formulation challenges in paediatric populations. Pharmaceutics 13. https://doi.org/10.3390/pharmaceutics13081114

Dimitri, P., Pignataro, V., Lupo, M., Bonifazi, D., Henke, M., Musazzi, U.M., Ernst, F., Minghetti, P., Redaelli, D.F., Antimisiaris, S.G., Migliaccio, G., Bonifazi, F., Marciani, L., Courtenay, A.J., Denora, N., Lopedota, A., 2021. Medical device development for children and young people—reviewing the challenges and opportunities. Pharmaceutics 13. https://doi.org/10.3390/pharmaceutics13122178

Dufour, G., Bigazzi, W., Wong, N., Boschini, F., De Tullio, P., Piel, G., Cataldo, D., Evrard, B., 2015. Interest of cyclodextrins in spray-dried microparticles formulation for sustained pulmonary delivery of budesonide. International Journal of Pharmaceutics 495, 869–878. https://doi.org/10.1016/j.ijpharm.2015.09.052

El Aita, I., Rahman, J., Breitkreutz, J., Quodbach, J., 2020a. 3D-Printing with precise layer-wise dose adjustments for paediatric use via pressure-assisted microsyringe printing. European Journal of Pharmaceutics and Biopharmaceutics 157, 59–65. https://doi.org/10.1016/j.ejpb.2020.09.012

El-Malah, Y., Nazzal, S., 2008. Effect of Eudragit® RS 30D and talc powder on verapamil hydrochloride release from beads coated with drug layered matrices. AAPS PharmSciTech 9, 75–83. https://doi.org/10.1208/s12249-007-9008-6

El-Say, K.M., Ahmed, T.A., Abdelbary, M.F., Ali, B.E., Aljaeid, B.M., Zidan, A.S., 2015. Risperidone oral disintegrating mini-tablets: A robust-product for pediatrics. Acta Pharmaceutica 65, 365–382. https://doi.org/10.1515/acph-2015-0038

Fang, S., Song, Y., Zhang, S., Li, C., 2019. Retrospective study of budesonide in children with eosinophilic gastroenteritis. Pediatric Research 86, 505–509. https://doi.org/10.1038/s41390-019-0444-2

Gao, C., Huang, J., Jiao, Y., Shan, L., Liu, Y., Li, Y., Mei, X., 2006. In vitro release and in vivo absorption in beagle dogs of meloxicam from Eudragit® FS 30 D-coated pellets. International Journal of Pharmaceutics 322, 104–112. https://doi.org/10.1016/j.ijpharm.2006.05.035

Gareb, B., Dijkstra, G., Kosterink, J.G.W., Frijlink, H.W., 2019. Development of novel zero-order release budesonide tablets for the treatment of ileo-colonic inflammatory bowel disease and comparison with formulations currently used in clinical practice. International Journal of Pharmaceutics 554, 366–375. https://doi.org/10.1016/j.ijpharm.2018.11.019

Goyanes, A., Allahham, N., Trenfield, S.J., Stoyanov, E., Gaisford, S., Basit, A.W., 2019. Direct powder extrusion 3D printing: Fabrication of drug products using a novel single-step process. International Journal of Pharmaceutics 567. https://doi.org/10.1016/j.ijpharm.2019.118471

Goyanes, A., Chang, H., Sedough, D., Hatton, G.B., Wang, J., Buanz, A., Gaisford, S., Basit, A.W., 2015. Fabrication of controlled-release budesonide tablets via desktop (FDM) 3D printing. International Journal of Pharmaceutics 496, 414–420. https://doi.org/10.1016/j.ijpharm.2015.10.039

Granados, P.A., Pinho, L.A.G., Sa-Barreto, L.L., Gratieri, T., Gelfuso, G.M., Cunha-Filho, M., 2022. Application of hot-melt extrusion in the complexation of naringenin with cyclodextrin using hydrophilic polymers. Advanced Powder Technology 33, 103380. https://doi.org/10.1016/j.apt.2021.11.032

Guajardo, J.R., Plotnick, L.M., Fende, J.M., Collins, M.H., Putnam, P.E., Rothenberg, M.E., 2002. Eosinophil-associated gastrointestinal disorders: A world-wide-web based registry. Journal of Pediatrics 141, 576–581. https://doi.org/10.1067/mpd.2002.127663

Herbada, R.S., Torres-Suárez, A.I., Otero-Espinar, F.J., Fraguas-Sanchez, A.I., Lopez-Cabarcos, E., Rubio-Retama, J., Fernández-Carballido, A., 2021. Matrix tablets based on a novel poly (magnesium acrylate) hydrogel for the treatment of inflammatory bowel diseases. International Journal of Pharmaceutics 608. https://doi.org/10.1016/j.ijpharm.2021.121121

Huyghebaert, N., Vermeire, A., Remon, J.P., 2004. Alternative method for enteric coating of HPMC capsules resulting in ready-to-use enteric-coated capsules. European Journal of Pharmaceutical Sciences 21, 617–623. https://doi.org/10.1016/j.ejps.2004.01.002

Illiger, S.R., Fadnis, C., Demappa, T., Jayaraju, J., Keshavayya, J., 2009. Miscibility studies of HPMC/PEG blends in water by viscosity, density, refractive index and ultrasonic velocity method. Carbohydrate Polymers 75, 484–488. https://doi.org/10.1016/j.carbpol.2008.08.014

Impellizzeri, G., Marasco, G., Eusebi, L.H., Salfi, N., Bazzoli, F., Zagari, R.M., 2019. Eosinophilic colitis: A clinical review. Digestive and Liver Disease 51, 769–773. https://doi.org/10.1016/j.dld.2019.04.011

Italian Official Pharmacopoeia XII edition, 2008a. Quality control of the preparation, Ist. Poligrafo dello Stato, pag.1421.

Italian Official Pharmacopoeia XII edition, 2008b. Friability of uncoated tablets, Ist. Poligrafo dello Stato, pag. 358.

Italian Official Pharmacopoeia XII edition, 2008c. Disaggregation assay of gastro-resistant tablets, Ist. Poligrafo dello Stato, pag. 893.

Italian Official Pharmacopoeia XII edition, 2008d. Recommended dissolution media, Ist. Poligrafo dello Stato, pagg. 351-352.

Jug, M., Mennini, N., Kövér, K.E., Mura, P., 2014. Comparative analysis of binary and ternary cyclodextrin complexes with econazole nitrate in solution and in solid state. Journal of Pharmaceutical and Biomedical Analysis 91, 81–91. https://doi.org/10.1016/j.jpba.2013.12.029

Kajiyama, A., Takagi, H., Moribe, K., Yamamoto, K., 2008. Improvement of HPMC tablet disintegration by the addition of inorganic salts. Chemical and Pharmaceutical Bulletin 56, 598–601. https://doi.org/10.1248/cpb.56.598

Kearns, G.L., Abdel-Rahman, S.M., Alander, S.W., Blowey, D.L., Leeder, J.S., Kauffman, R.E., 2003. Developmental Pharmacology — Drug Disposition, Action, and Therapy in Infants and Children. New England Journal of Medicine 349, 1157–1167. https://doi.org/10.1056/nejmra035092

Kim, J.E., Cho, H.J., Kim, D.D., 2014. Budesonide/cyclodextrin complex-loaded lyophilized microparticles for intranasal application. Drug Development and Industrial Pharmacy 40, 743–748. https://doi.org/10.3109/03639045.2013.782503

Kinnarinen, T., Jarho, P., Järvinen, K., Järvinen, T., 2003. Pulmonary deposition of a budesonide/γ-cyclodextrin complex in vitro. Journal of Controlled Release 90, 197–205. https://doi.org/10.1016/S0168-3659(03)00176-7

Kuźmińska, M., Pereira, B.C., Habashy, R., Peak, M., Isreb, M., Gough, T.D., Isreb, A., Alhnan, M.A., 2021. Solvent-free temperature-facilitated direct extrusion 3D printing for pharmaceuticals. International Journal of Pharmaceutics 598, 1–9. https://doi.org/10.1016/j.ijpharm.2021.120305

Lafeber, I., Ruijgrok, E.J., Guchelaar, H.J., Schimmel, K.J.M., 2022a. 3D Printing of Pediatric Medication: The End of Bad Tasting Oral Liquids? —A Scoping Review. Pharmaceutics 14, 1–23. https://doi.org/10.3390/pharmaceutics14020416

Laquintana, V., Asim, M.H., Lopedota, A., Cutrignelli, A., Lopalco, A., Franco, M., Bernkop-Schnürch, A., Denora, N., 2019b. Thiolated hydroxypropyl-β-cyclodextrin as mucoadhesive excipient for oral delivery of budesonide in liquid paediatric formulation. International Journal of Pharmaceutics 572, 118820. https://doi.org/10.1016/j.ijpharm.2019.118820

Letmanski, T., Kodym, A., Weber, P., Lewandowski, M., Wisniewski, A., Baj, T., 2015. Eudragit FS 30D as a potential polymer for use in the technology of preparing matrix tablets contain metronidazole - An experimental and mathematical modeling study. Current Issues in Pharmacy and Medical Sciences 28, 97–104. https://doi.org/10.1515/cipms-2015-0053

Liao, Q., Lam, I.C.H., Lin, H.H.S., Wan, L.T.L., Lo, J.C.K., Tai, W., Kwok, P.C.L., Lam, J.K.W., 2020. Effect of formulation and inhaler parameters on the dispersion of spray freeze dried voriconazole particles. International Journal of Pharmaceutics 584. https://doi.org/10.1016/j.ijpharm.2020.119444

Licari, A., Votto, M., D’Auria, E., Castagnoli, R., Caimmi, S.M.E., Marseglia, G.L., 2019. Eosinophilic Gastrointestinal Diseases in Children: A Practical Review. Current Pediatric Reviews 16, 106–114. https://doi.org/10.2174/1573396315666191022154432

Lima, A.L., Pinho, L.A.G., Chaker, J.A., Sa-Barreto, L.L., Marreto, R.N., Gratieri, T., Gelfuso, G.M., Cunha-Filho, M., 2020. Hot-melt extrusion as an advantageous technology to obtain effervescent drug products. Pharmaceutics 12, 1–20. https://doi.org/10.3390/pharmaceutics12080779

Liu, S., Yu, J., Zou, J., Yang, Y., Cui, L., Chang, X., 2020. Effects of different drying and milling methods on the physicochemical properties and phenolic content of hawthorn fruit powders. Journal of Food Processing and Preservation 44. https://doi.org/10.1111/jfpp.14460

Loftsson, T., Másson, M., Sigurjónsdóttir, J.F., 1999. Methods to enhance the complexation efficiency of cyclodextrins. S.T.P. Pharma Sciences 9, 237–242.

Londhe, V.Y., Pawar, A., Kundaikar, H., 2020. Studies on spectral characterization and solubility of hydroxypropyl β-cyclodextrin/iloperidone binary and ternary complexes using different auxiliary agents. Journal of Molecular Structure 1220. https://doi.org/10.1016/j.molstruc.2020.128615

Lozinsky, A.C., Morais, M.B. De, 2014. Eosinophilic colitis in infants. Jornal de Pediatria 90, 16–21. https://doi.org/10.1016/j.jped.2013.03.024

Lucendo, A.J., Serrano-Montalbán, B., Arias, Á., Redondo, O., Tenias, J.M., 2015. Efficacy of Dietary Treatment for Inducing Disease Remission in Eosinophilic Gastroenteritis. Journal of Pediatric Gastroenterology and Nutrition 61, 56–64. https://doi.org/10.1097/MPG.0000000000000766

Maejima, T., McGinity, J.W., 2001. Influence of film additives on stabilizing drug release rates from pellets coated with acrylic polymers. Pharmaceutical Development and Technology 6, 211–221. https://doi.org/10.1081/PDT-100002197

Magro, F., Cordeiro, G., Dias, A.M., Estevinho, M.M., 2020. Inflammatory Bowel Disease – Non-biological treatment. Pharmacological Research 160. https://doi.org/10.1016/j.phrs.2020.105075

Malaquias, L.F.B., Sá-Barreto, L.C.L., Freire, D.O., Silva, I.C.R., Karan, K., Durig, T., Lima, E.M., Marreto, R.N., Gelfuso, G.M., Gratieri, T., Cunha-Filho, M., 2018. Taste masking and rheology improvement of drug complexed with beta-cyclodextrin and hydroxypropyl-β-cyclodextrin by hot-melt extrusion. Carbohydrate Polymers 185, 19–26. https://doi.org/10.1016/j.carbpol.2018.01.011

Mali, A.J., Pawar, A.P., Purohit, R.N., 2014. Development of Budesonide Loaded Biopolymer Based Dry Powder Inhaler: Optimization, In Vitro Deposition, and Cytotoxicity Study . Journal of Pharmaceutics 2014, 1–12. https://doi.org/10.1155/2014/795371

Maroni, A., Zema, L., Cerea, M., Foppoli, A., Palugan, L., Gazzaniga, A., 2016. Erodible drug delivery systems for time-controlled release into the gastrointestinal tract. Journal of Drug Delivery Science and Technology 32, 229–235. https://doi.org/10.1016/j.jddst.2015.10.001

Medarević, D., Kachrimanis, K., Djurić, Z., Ibrić, S., 2015. Influence of hydrophilic polymers on the complexation of carbamazepine with hydroxypropyl-β-cyclodextrin. European Journal of Pharmaceutical Sciences 78, 273–285. https://doi.org/10.1016/j.ejps.2015.08.001

Melton, G.B., Gaertner, W.B., MacDonald, J.E., Kwaan, M.R., Shepela, C., Madoff, R., Jessurun, J., 2011. Eosinophilic colitis: University of Minnesota experience and literature review. Gastroenterology Research and Practice 2011. https://doi.org/10.1155/2011/857508

Michailidou, G., Papageorgiou, G.Z., Bikiaris, D.N., 2021. β-Cyclodextrin Inclusion Complexes of Budesonide with Enhanced Bioavailability for COPD Treatment. Applied Sciences (Switzerland) 11. https://doi.org/10.3390/app112412085

Mirdamadian, S.Z., Varshosaz, J., Minaiyan, M., Taheri, A., 2022. 3D printed tablets containing oxaliplatin loaded alginate nanoparticles for colon cancer targeted delivery. An in vitro/in vivo study. International Journal of Biological Macromolecules 205, 90–109. https://doi.org/10.1016/j.ijbiomac.2022.02.080

Moghimipour, E., Rezaei, M., Kouchak, M., Fatahiasl, J., Angali, K.A., Ramezani, Z., Amini, M., Dorkoosh, F.A., Handali, S., 2018. Effects of coating layer and release medium on release profile from coated capsules with Eudragit FS 30D: an in vitro and in vivo study. Drug Development and Industrial Pharmacy 44, 861–867. https://doi.org/10.1080/03639045.2017.1415927

Ozdemir, N., Pola, C.C., Teixeira, B.N., Hill, L.E., Bayrak, A., Gomes, C.L., 2018. Preparation of black pepper oleoresin inclusion complexes based on beta-cyclodextrin for antioxidant and antimicrobial delivery applications using kneading and freeze-drying methods: A comparative study. LWT - Food Science and Technology 91, 439–445. https://doi.org/10.1016/j.lwt.2018.01.046

Page, S., Maurer, R., Wyttenbach, N., 2016. Structured development approach for amorphous systems. AAPS Advances in the Pharmaceutical Sciences Series 22, 329–382. https://doi.org/10.1007/978-3-319-42609-9_8

Palugan, L., Filippin, I., Cirilli, M., Moutaharrik, S., Zema, L., Cerea, M., Maroni, A., Foppoli, A., Gazzaniga, A., 2021. Cellulase as an “active” excipient in prolonged-release HPMC matrices: A novel strategy towards zero-order release kinetics. International Journal of Pharmaceutics 607, 121005. https://doi.org/10.1016/j.ijpharm.2021.121005

Patel, A.R., Vavia, P.R., 2008. Preparation and evaluation of taste masked famotidine formulation using drug/β-cyclodextrin/polymer ternary complexation approach. AAPS PharmSciTech 9, 544–550. https://doi.org/10.1208/s12249-008-9078-0

Pereira, M.N., Schulte, H.L., Duarte, N., Lima, E.M., Sá-Barreto, L.L., Gratieri, T., Gelfuso, G.M., Cunha-Filho, M.S.S., 2017. Solid effervescent formulations as new approach for topical minoxidil delivery. European Journal of Pharmaceutical Sciences 96, 411–419. https://doi.org/10.1016/j.ejps.2016.10.016

Pistone, M., Racaniello, G.F., Arduino, I., Laquintana, V., Lopalco, A., Cutrignelli, A., Rizzi, R., Franco, M., Lopedota, A., Denora, N., 2022. Direct cyclodextrin-based powder extrusion 3D printing for one-step production of the BCS class II model drug niclosamide. Drug Delivery and Translational Research. https://doi.org/10.1007/s13346-022-01124-7

Poller, B., Strachan, C., Broadbent, R., Walker, G.F., 2017. A minitablet formulation made from electrospun nanofibers. European Journal of Pharmaceutics and Biopharmaceutics 114, 213–220. https://doi.org/10.1016/j.ejpb.2017.01.022

Pose-Vilarnovo, B., Rodríguez-Tenreiro, C., Rosa Dos Santos, J.F., Vázquez-Doval, J., Concheiro, A., Alvarez-Lorenzo, C., Torres-Labandeira, J.J., 2004. Modulating drug release with cyclodextrins in hydroxypropyl methylcellulose gels and tablets. Journal of Controlled Release 94, 351–363. https://doi.org/10.1016/j.jconrel.2003.10.002

Rabito, M.F., Reis, A.V., Reis Freitas, A. Dos, Tambourgi, E.B., Cavalcanti, O.A., 2012. A pH/enzyme-responsive polymer film consisting of Eudragit® FS 30 D and arabinoxylane as a potential material formulation for colon-specific drug delivery system. Pharmaceutical Development and Technology 17, 429–436. https://doi.org/10.3109/10837450.2010.546409

Rakkaew, P., Suksiriworapong, J., Chantasart, D., 2018. β-Cyclodextrin-based ternary complexes of haloperidol and organic acids: the effect of organic acids on the drug solubility enhancement. Pharmaceutical Development and Technology 23, 715–722. https://doi.org/10.1080/10837450.2017.1344993

Redenti, E., Szente, L., Szejtli, J., 2000. Drug/cyclodextrin/hydroxy acid multicomponent systems. Properties and pharmaceutical applications. Journal of Pharmaceutical Sciences 89, 1–8. https://doi.org/10.1002/(SICI)1520-6017(200001)89:1<1:AID-JPS1>3.0.CO;2-W

Ribeiro, L.S.S., Ferreira, D.C., Veiga, F.J.B., 2003. Physicochemical investigation of the effects of water-soluble polymers on vinpocetine complexation with β-cyclodextrin and its sulfobutyl ether derivative in solution and solid state. European Journal of Pharmaceutical Sciences 20, 253–266. https://doi.org/10.1016/S0928-0987(03)00199-4

Sánchez-Guirales, S.A., Jurado, N., Kara, A., Lalatsa, A., Serrano, D.R., 2021. Understanding direct powder extrusion for fabrication of 3d printed personalised medicines: A case study for nifedipine minitablets. Pharmaceutics 13. https://doi.org/10.3390/pharmaceutics13101583

Santos Akkari, A.C., Ramos Campos, E.V., Keppler, A.F., Fraceto, L.F., de Paula, E., Tófoli, G.R., de Araujo, D.R., 2016. Budesonide-hydroxypropyl-β-cyclodextrin inclusion complex in binary poloxamer 407/403 system for ulcerative colitis treatment: A physico-chemical study from micelles to hydrogels. Colloids and Surfaces B: Biointerfaces 138, 138–147. https://doi.org/10.1016/j.colsurfb.2015.11.048

Santos, E.H., Kamimura, J.A., Hill, L.E., Gomes, C.L., 2015. Characterization of carvacrol beta-cyclodextrin inclusion complexes as delivery systems for antibacterial and antioxidant applications. LWT - Food Science and Technology 60, 583–592. https://doi.org/10.1016/j.lwt.2014.08.046

Saokham, P., Burapapadh, K., Praphanwittaya, P., Loftsson, T., 2020. Characterization and evaluation of ternary complexes of ascorbic acid with γ-cyclodextrin and poly(Vinyl alcohol). International Journal of Molecular Sciences 21, 1–14. https://doi.org/10.3390/ijms21124399

Scoutaris, N., Ross, S.A., Douroumis, D., 2018. 3D Printed “Starmix” Drug Loaded Dosage Forms for Paediatric Applications. Pharmaceutical Research 35, 1–11. https://doi.org/10.1007/s11095-017-2284-2

Siepmann, J., Peppas, N.A., 2012. Modeling of drug release from delivery systems based on hydroxypropyl methylcellulose (HPMC). Advanced Drug Delivery Reviews 64, 163–174. https://doi.org/10.1016/j.addr.2012.09.028

Soltani, F., Kamali, H., Akhgari, A., Garekani, H.A., Nokhodchi, A., Sadeghi, F., 2022. Different trends for preparation of budesonide pellets with enhanced dissolution rate. Advanced Powder Technology 33, 103684. https://doi.org/10.1016/j.apt.2022.103684

Stato, P. di, n.d. Italian Official Pharmacopoeia XII edition.

Suárez-González, J., Magariños-Triviño, M., Díaz-Torres, E., Cáceres-Pérez, A.R., Santoveña-Estévez, A., Fariña, J.B., 2021. Individualized orodispersible pediatric dosage forms obtained by molding and semi-solid extrusion by 3D printing: A comparative study for hydrochlorothiazide. Journal of Drug Delivery Science and Technology 66. https://doi.org/10.1016/j.jddst.2021.102884

Sun, H., Wang, X., Wang, J., Shi, G., Chen, L., 2020. Influence of the formula on the properties of a fast dispersible fruit tablet made from mango, Chlorella, and cactus powder. Food Science and Nutrition 8, 479–488. https://doi.org/10.1002/fsn3.1330

Takano, R., Maurer, R., Jacob, L., Stowasser, F., Stillhart, C., Page, S., 2020. Formulating Amorphous Solid Dispersions: Impact of Inorganic Salts on Drug Release from Tablets Containing Itraconazole-HPMC Extrudate. Molecular Pharmaceutics 17, 2768–2778. https://doi.org/10.1021/acs.molpharmaceut.9b01109

Thakral, N., Ray, A.R., Shalom, D.B., Eriksson, A.H., Majumdar, D., 2011. The quest for targeted delivery in colon cancer: mucoadhesive valdecoxib microspheres. International Journal of Nanomedicine 1057. https://doi.org/10.2147/IJN.S19561

Thiry, J., Krier, F., Ratwatte, S., Thomassin, J.M., Jerome, C., Evrard, B., 2017. Hot-melt extrusion as a continuous manufacturing process to form ternary cyclodextrin inclusion complexes. European Journal of Pharmaceutical Sciences 96, 590–597. https://doi.org/10.1016/j.ejps.2016.09.032

Wang, N.W., Hsieh, H., Yang, Y.J., 2021. Successful Montelukast Treatment in an Infant with Steroid-Resistant Eosinophilic Colitis. Case Reports in Gastroenterology 15, 389–394. https://doi.org/10.1159/000513146

Wang, Y., Grohganz, H., Rades, T., 2022. Effects of polymer addition on the non-strongly interacting binary co-amorphous system carvedilol-tryptophan. International Journal of Pharmaceutics 617, 121625. https://doi.org/10.1016/j.ijpharm.2022.121625

Wesseling, M., Kuppler, F., Bodmeier, R., 1999. Tackiness of acrylic and cellulosic polymer films used in the coating of solid dosage forms. European Journal of Pharmaceutics and Biopharmaceutics 47, 73–78. https://doi.org/10.1016/S0939-6411(98)00091-5

Wu, C., McGinity, J.W., 2003. Influence of an enteric polymer on drug release rates of theophylline from pellets coated with Eudragit® RS 30D. Pharmaceutical Development and Technology 8, 103–110. https://doi.org/10.1081/PDT-120017529

Xi, H., Ren, J., Novak, J.M., Kemp, E., Johnson, G., Klinzing, G., Johnson, M.A., Xu, W., 2020. The Effect of Inorganic Salt on Disintegration of Tablets with High Loading of Amorphous Solid Dispersion Containing Copovidone. Pharmaceutical Research 37. https://doi.org/10.1007/s11095-020-2772-7

Yan, Y., Wang, P., Li, R., Sun, Y., Zhang, R., Huo, C., Xing, J., Dong, Y., 2019. Synthesis of budesonide conjugates and their anti-inflammatory effects: A preliminary study. Drug Design, Development and Therapy 13, 681–694. https://doi.org/10.2147/DDDT.S192348

Yuan, C., Liu, B., Liu, H., 2015. Characterization of hydroxypropyl-β-cyclodextrins with different substitution patterns via FTIR, GC-MS, and TG-DTA. Carbohydrate Polymers 118, 36–40. https://doi.org/10.1016/j.carbpol.2014.10.070

Zema, L., Melocchi, A., Maroni, A., Gazzaniga, A., 2017. Three-Dimensional Printing of Medicinal Products and the Challenge of Personalized Therapy. Journal of Pharmaceutical Sciences 106, 1697–1705. https://doi.org/10.1016/j.xphs.2017.03.021

Zhao, J., Yin, D., Rowe, J., Badawy, S., Nikfar, F., Pandey, P., 2018. Understanding the Factors That Control the Quality of Mini-Tablet Compression: Flow, Particle Size, and Tooling Dimension. Journal of Pharmaceutical Sciences 107, 1204–1208. https://doi.org/10.1016/j.xphs.2017.12.002

Zuccari, G., Alfei, S., Marimpietri, D., Iurilli, V., Barabino, P., Marchitto, L., 2022. Mini-Tablets: A Valid Strategy to Combine Efficacy and Safety in Pediatrics. Pharmaceuticals 15. https://doi.org/10.3390/ph15010108